## Slide 2
I. Manual screening
  Engineering judgment
  Process Knowledge
II. Unsupervised screening
  Trajectory similarity
  Clustering
III. Modeling and statistical analysis
  Based on output correlation
IV. Model refinement and validation
  Refine model and isolate variable
If unsatisfactory

## Slide 4: IV. 2nd stage PLS model
The wafer to wafer variations are not very well captured
but lot-to-lot variations are being predicted
Results

## Slide 7: Model Refinement: Dynamic PLS model
Includes lagged values of yk-1, yk-2 into the X matrix
R2corr = 0.9258
R2test = 0.9020
Normalized Rs
Normalized Rs
Wafer Samples
Blue line – prediction
Circles – measurements
Colored by lot ID
Results

## Slide 8: Model Refinement – Time Series Residual
R2test = 0.8370
R2train = 0.9136
an ARMA(1,1) time series model was found to be sufficient
Normalized Rs
Normalized Rs
Wafer Samples
Blue line – prediction
Circles – measurements
Colored by lot ID
Results

## Slide 9: Score plot of the reduced model
The testing data (shaded squares) are within the valid operating regime
Colored by device ID
Results

## Slide 10: Relevant samples from batch trajectory
Results
Notes: Most of the signals do not show significant variation during the time range of interest
Summarize by mean, then successively add other statistical moments to see if they improve the model performance

## Slide 11: Models using summary data
 | Number of Parameters | Model Description | R2 training | R2 testing
1 | 36 | Raw trace + lagged y | 0.9258 | 0.9020
2 | 8 | Mean | 0.6737 | 0.6903
3 | 16 | Mean + std | 0.7202 | -0.5774
4 | 16 | Mean + max | 0.6841 | 0.6801
5 | 16 | Mean + sum (integral) | 0.6737 | 0.6903
6 | 16 | Mean + derivative | 0.6882 | 0. 5880
7 | 10 | Mean + lagged y | 0.9231 | 0.9138
Blue line – prediction
Circles – measurements
Colored by lot ID
Results

## Slide 12
Ar Flow (sccm) | ChuckESCCurrentMonitor2Reading (uAmp) | N2 Flow (sccm)
BiasMatchSeriesCapPositionAIReading (count) | ChuckESCTotalVoltageReading (V) | OESB1Value
BiasMatchShuntCapPositionAIReading (count) | ChuckHeBacksidePressureReading (torr) | PreviousStepElapsedProcessTime (s)
BiasRFCurrentProbeAIReading (amp) | ChuckRFVoltageProbeAIReading (V) | ProcessManometerAdjustedPressure
BiasRFGenForwardPowerAIReading (watt) | Cl2 Flow (sccm) | TCPMatchC1CapPositionAIReading (count)
BiasRFGenReflectedPowerAIReading (watt) | CurrentStepNumber | TCPMatchC3CapPositionAIReading (count)
BiasRFVoltageProbeAIReading (V) | ForelinePressureManometer | TCPRFGenReflectedPowerAIReading (watt)
ChuckESCBiasVoltageReading (V) | HeInnerZoneBacksideFlow | TemperatureControlESCTargetFlowSensorReading (GPM)
ChuckESCCurrentMonitor1Reading (uAmp) | Manometer | ThrottleValvePosition
This list of variables are manually screened from a list of 100 signals in FabGuard. Subsequent screening of variables are based on data based methods
Appendices

## Slide 13: Appendix: Variables that are not relevant to the process
Ar Flow (sccm); SVID21800731'
BiasMatchSeriesCapPositionAIReading (count); SVID21800070'
BiasRFCurrentProbeAIReading (amp); SVID21800678'
BiasRFGenForwardPowerAIReading (watt); SVID21800092'
BiasRFGenReflectedPowerAIReading (watt); SVID21800097'
BiasRFVoltageProbeAIReading (V); SVID21800679'
ChuckESCTotalVoltageReading (V); SVID21800229'
ChuckHeBacksidePressureReading (torr); SVID21800237'
ChuckRFVoltageProbeAIReading (V); SVID21800961'
Cl2 Flow (sccm); SVID21800701'
CurrentStepNumber; SVID21800003 [Tool''s Step]'
ForelinePressureManometer; SVID21800883'
HeInnerZoneBacksideFlow; SVID21800236'
Manometer; SVID21800873'
PreviousStepElapsedProcessTime (s); SVID21802475'
ProcessManometerAdjustedPressure; SVID21800870'
TCPMatchC1CapPositionAIReading (count); SVID21800186'
TCPMatchC3CapPositionAIReading (count); SVID21800197'
TCPRFGenReflectedPowerAIReading (watt); SVID21800217'
TemperatureControlESCTargetFlowSensorReading (GPM); SVID21800894'
ThrottleValvePosition; SVID21800437'
Appendices

## Slide 14: Appendix: Variables removed due to poor excitation (no variation)
37 – Bias ESC capacitance
35 – Nitrogen purge flow
52 – Dry Pump Temperature
53 – Dry Pump motor temperature
54 – Dry Pump oil status
55 – Dry Pump Phase Current
56 – Dry Pump Power
66 – Inverter Current
63 – Hours on Process
68 – Inverter speed
69 – Inverter Torque
71 – Booster Pump Motor Temp
73 – Booster Pump Phase Current
74 – Booster Pump Power ( meaningless oscillations)
80 – Cycles
82 – Pump system cycles
86 - Tool: TCPRFGenForwardPowerAIReading (watt); SVID21800212
88 - TemperatureControlChamberAverageTemperatureReading
89 - TemperatureControlESCTargetCurrentSetpoint
91 - TemperatureControlESCTargetTemperatureSensorReading
Appendices

## Slide 15: Appendix: traces removed due to lack of data (incomplete or over 50% missing)
Shaft-seals Purge Pressure (kPa)
Mechanical Booster Pump Oil Status
Latch: N2 Setpoint; SVID21800820
Sig: N2 Flow Deviation
Sig: Previous Step Number
Sig: Run Time
Sig: TCP Power Deviation
Sig: TCP Reflected Power Ratio
Tool Bin Data Age
Tool Bin Polling Latency
Tool: Active Gauge Pressure (Pa); EdwardsD372:7,53
Tool: Analog Water Flow (ml/s); EdwardsD372:7,52
Tool: Electrical Supply Voltage (V); EdwardsD372:7,2
Tool: Exhaust Temperature (K); EdwardsD372:7,56
Tool: Final Stage Purge Nitrogen Flow (ml/s); EdwardsD372:7,32
Tool: Imbalance in Dry Pump Phase Current (%); EdwardsD372:7,6
Tool: Imbalance in Mechanical Booster Pump Phase Current (%); EdwardsD372:7,10
Tool: Inverter Power (kW); EdwardsD372:7,173
Appendices